## Slide 1
Reduce Scrap at the Extrusion
DMAIC
Plastec-Stream

## Slide 2
DMAIC

## Slide 3
DMAIC
Grinder
Regrind
SILOS
Regrind
Polystyrene
Color Concentrate
Feeders
Winder
S-wrap
Mandrel
Die/
Air Ring
Primary Extruder
Secondary Extruder
Screen
Butane
Blender
Foam Rollstock
Testing

## Slide 4
Project Progress Overview
D1.Project Charter
Problem statement.
Primary Metric
Goal statement
Purpose and scope
Team
D2 SIPOC
D3 CTQ: Roll stock Specs
M0 Measure outcomes
M1.Extrusion Current Process Map
M21 Summary of descriptive statistics on daily Extrusion scrap
M22 Control charts
M3 Actual yield, cost and process sigma and goals.
M41 Extrusion Scrap per cause
M42 Causes Tree Diagram
A0 Analyze outcomes
A1 Detailed process map
A2 Vital Few Identification
Pareto and Regression Analysis
A31 T- test conclusion
A32 Hypothesis test on Vital
Few Causes
A33 Root Cause Analysis
Fishbone Diagram
A4 List of Identified and verified main root causes of scrap.
I0 Improve outcomes
I1 Possible solutions to verified root causes.
I2 Evaluate and select
best solution(low
risk/high reward)
I3 Pilot and test solutions.
Actual key perf.indicator Vs baseline test
I4.Implement the optimized process model.
C0 Control outcomes
C1. Sustain the improvement:
control and monitoring plan:
control chart
Key Deliverables:
Project Charter
Key performance indicator
Defined goal
Project timeline
Baseline calculation.
Target performance outputs calculation.
Identify all x causing problems.
Vital few causes
Cause and Effect results.
Regression model
Optimal solution.
Pilot and test.
Implementation
Monitoring and control.
Ownership
Milestone:
Planned
Completed
1/4/2014
1/26/2014
2/16/2014
3/16/2014
4/6/2014
1/25/2014
2/15/2014
3/15/2014
4/5/2014
5/26/2014
Steps:
Tools:
Project charter.
SIPOC
CTQ Tree diagram.
Daily scrap data
Descriptive statistics.
Control chart
Capability analysis
Brainstorming
Process map
Detailed process map
Pareto analysis
Regression Analysis
Hypothesis test.
Fishbone/5 Whys
Brainstorming
Impact/Effort & cost Matrix
Descriptive statistics
Control chart.
Capability study.
Control plan.
Visual management tools
Mistake proof methods
Control Charts
SOP/ODS
Define
Measure
Analyze
Improve
Control
Roadmap
Day | 21 | 21 | 28 | 21 | 21
Cumulative(%) | 18.75 | 37.50 | 62.50 | 81.25 | 100.00
Time and progress:
Notes: Update your dates. This is intended to give you ideas for tool selection.

## Slide 5
In Scope:
Extrusion Department
Defect:
Rollstock scrap.
Metric :LBS rollstock scrap per day
Business Case:
Plastec-Stream Inc ,a packaging company that mainly produce egg cartons, has an excessive amount of rollstock sheet scrap at the Extrusion department.
This create a loss in raw materials and a big challenge on delivering on time customer orders.
Problem Statement:
Manufacturing and delivering on time egg cartons can
not be sustained with the tremendous amount of scrap(Average 3,326 LBS/day) which cost more than
$3,357 per day or $1,208,520 a year.
Goal Statement:
Reduce Extrusion line daily scrap from 3,325 LBS to 1500 LBS by end of June 2014 for a saving of $544,320 a year.
Start / Stop Points for Project:
Extrusion Silos /Extrusion S-wrap Station
Define - Step D1
Team/Key Stakeholder.
Ben Williamson Plant Manager Sponsor
Dennis Prayer QA Manager Champion
Ted Davis Extrusion Mgr Subject Expert
Donatien Toni Lean Six Sigma Black Belt
Sipola Ongewe Lean Six Sigma Black Belt
Project Charter
Notes: 1. Verify importance of problem and project with your Champion(s)
Discuss the goal and scope of the project with your Champion(s)
Determine project pace and update the cover page
Remember that your Charter page is a “living” document and CHANGES as you go through D-M-A-I-C and gather your data. In Step 2 of Measure we’ll “lock-in” these measures. As you complete your project, you should modify this page to reflect what you learn about your problem.

## Slide 6
Define - Step D2
Extrusion SIPOC Map
SIPOC |  |  |  |  |  |  |  |  |  |  | 
Suppliers |  | Inputs |  | Process |  | Outputs |  | Customers |  | Requirements | 
 |  |  |  | Blender |  |  |  |  |  |  | 
 |  |  |  | Screws |  |  |  |  |  | Segment Weight | 
 |  | Crystal Polystrene |  |  |  |  |  |  |  |  | 
Raw materials |  | Virgin |  |  |  |  |  | Forming |  | Thickness | 
Suppliers |  | Color |  | Die |  | Foam sheet (Rollstock) |  |  |  |  | 
 |  | Talc |  |  |  |  |  |  |  | Cell size | 
 |  | Butane |  |  |  |  |  | Printing |  |  | 
 |  |  |  | Mandrel |  |  |  |  |  | Color | 
Grinders |  | Regrind |  |  |  |  |  |  |  | Orientation | 
 |  |  |  | S-wrap |  |  |  |  |  |  | 
 |  |  |  | Winder |  |  |  |  |  | In specs | 
External Customers

## Slide 7: Outcome of Measure Phase
The Goal of Measure Phase – To establish current baseline:
  Current Process Map
  Descriptive Statistics
    Daily Scrap Average
    Daily Prime Average
  Variation Analysis
    Can we trust data we obtain from the process?
  Determine Process Capability
    Can we produce a product which will meet the customers tolerances?
  Scrap per cause
    Identify our baseline list of scrap causes
Measure-Step M0

## Slide 8
Measure-Step M1
Baseline
Extrusion Current Process Map
Notes: 1. Addresses: What Does the Customer Want? What is a Good Product/Process? What is a Defect?
2. Goal of Performance Standard is to Translate the Customer Need into a MEASURABLE Characteristic.
3. Operational Definition is a Precise Description that Tells How to get a Value for the Characteristic You are Measuring.
To add or delete rows within this table, right-click and select “insert rows” or “delete rows”.

## Slide 9
Measure-Step M21
Baseline Statistics
Extrusion daily yield
Date Prime Scrap Yield
10/1/13 55536 3594 93.5
10/2/13 58973 3159 94.6
10/3/13 39053 1418 96.4
10/4/13 41844 2793 93.3
10/5/13 58659 2116 96.4
10/6/13 55753 1278 97.7
10/7/13 43299 3614 91.7
10/8/13 45082 2615 94.2
10/9/13 63920 2225 96.5
10/11/13 47917 5416 88.7
10/12/13 60870 881 98.6
10/13/13 63668 2282 96.4
10/14/13 63527 972 98.5
10/15/13 47258 1524 96.8
10/16/13 36006 2315 93.6
10/17/13 48245 3186 93.4
10/18/13 50529 6793 86.6
10/19/13 44889 1278 97.2
Mean daily Scrap = 3,326 LBS
Mean daily prime = 53,536 LBS
N=103
Period = 10/1/2013 thru 1/24/2014
Notes: 1. Addresses: What Does the Customer Want? What is a Good Product/Process? What is a Defect?
2. Goal of Performance Standard is to Translate the Customer Need into a MEASURABLE Characteristic.
3. Operational Definition is a Precise Description that Tells How to get a Value for the Characteristic You are Measuring.
To add or delete rows within this table, right-click and select “insert rows” or “delete rows”.

## Slide 10
Variation Analysis
  IMR charts determined that the process variation is in control
Process Capability
  Cpk was calculated at 0.64
  Well below expected
Baseline on Extrusion Daily Scrap
Measure-Step M22

## Slide 11
Measure-Step M3
Baseline on yield, cost and goals
Actual/Goal
Notes: 1. Addresses: What Does the Customer Want? What is a Good Product/Process? What is a Defect?
2. Goal of Performance Standard is to Translate the Customer Need into a MEASURABLE Characteristic.
3. Operational Definition is a Precise Description that Tells How to get a Value for the Characteristic You are Measuring.
To add or delete rows within this table, right-click and select “insert rows” or “delete rows”.

## Slide 12
Measure-Step M42
Causes Tree Diagram
 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | SCRAP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Color Change |  |  |  | Mechanical |  |  |  | Start Up |  |  |  | Contaminated |  |  |  | Out of Spec |  |  |  | Feed Syst. |  |  |  | Trash in Die |  |  |  | Break Out |  |  |  | Butane Issues |  |  |  | Runout of |  |  |  | Runout of |  |  |  | Runout of |  |  |  | Shutdouwn |  | 
CC |  |  |  | MECH |  |  |  | SU |  |  |  | Regrind(CR) |  |  |  | OS |  |  |  | Failure(FSF) |  |  |  | TD |  |  |  | BO |  |  |  | BI |  |  |  | Regrind(RR) |  |  |  | Virgin(RV) |  |  |  | Color(RC) |  |  |  | SD |  | 
Change over |  |  |  | Screens |  |  |  | Inventory |  |  |  | Different |  |  |  | 4.5 RPM |  |  |  | Low Light |  |  |  | CR |  |  |  | Trash |  |  |  | Not at setpoint |  |  |  | Low light |  |  |  | Clumps in |  |  |  |  |  |  |  | Inventory |  | 
CO |  |  |  | Heaters |  |  |  | Maint. |  |  |  | regrind color |  |  |  | Blade dull |  |  |  | Compressed |  |  |  |  |  |  |  | Dirty Mandrel |  |  |  | Pump |  |  |  | not working |  |  |  | Hopper |  |  |  |  |  |  |  | Maintenance |  | 
CR |  |  |  | Mandrel |  |  |  | Unschedule |  |  |  | Trash |  |  |  | Spots on |  |  |  | air |  |  |  |  |  |  |  | Water flow |  |  |  |  |  |  |  | Empty Silos |  |  |  | Feeder Stop |  |  |  |  |  |  |  | Unschedule |  | 
FSF |  |  |  | Water flow |  |  |  | shutdown |  |  |  | Water |  |  |  | Sheet |  |  |  | Auger |  |  |  |  |  |  |  | Electrical |  |  |  |  |  |  |  | Jams |  |  |  | Compressed |  |  |  |  |  |  |  | shutdown |  | 
RR |  |  |  | Valve |  |  |  | Power out |  |  |  |  |  |  |  | 4.5 Amps |  |  |  | Feeder |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Clumps |  |  |  | air |  |  |  | ` |  |  |  | Power out |  | 
RC |  |  |  | Compressed |  |  |  |  |  |  |  |  |  |  |  | Operator |  |  |  | Pump |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Trash |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Operator |  |  |  | air |  |  |  |  |  |  |  |  |  |  |  | Water flow |  |  |  | Shaker |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Operator |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Colorator |  |  |  | 4.5 RPM |  |  |  |  |  |  |  |  |  |  |  | Pressure |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Compressed |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  | 4.5 AMPS |  |  |  |  |  |  |  |  |  |  |  | Butane |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | air |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  | Power out |  |  |  |  |  |  |  |  |  |  |  | S-wrap Speed |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Bent auger |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  | Feeder |  |  |  |  |  |  |  |  |  |  |  | Talc Feeder |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Power out |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  | pump |  |  |  |  |  |  |  |  |  |  |  | Die Gap |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Feeder pump |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  | Die |  |  |  |  |  |  |  |  |  |  |  | CC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  | Air ring |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  | Water leak |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  | Die /mandrel |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  | change |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  | Colorator |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Extrusion Scrap per Cause
Notes: 1. Addresses: What Does the Customer Want? What is a Good Product/Process? What is a Defect?
2. Goal of Performance Standard is to Translate the Customer Need into a MEASURABLE Characteristic.
3. Operational Definition is a Precise Description that Tells How to get a Value for the Characteristic You are Measuring.
To add or delete rows within this table, right-click and select “insert rows” or “delete rows”.

## Slide 13: Outcome of Analyze Phase
Our Objective is to narrow to the vital few
  By looking at each step and seeing where the problems are originating from.
    Detailed Process Map with root cause analysis
  By narrowing down to the vital few using the following tools.
    Pareto Analysis – 80 percent of our Scrap was produced by 20% of the causes
      6 key causes identified
    Regression Analysis – Proved that the six identified were significant
    Hypothesis Testing – The vital few were identified (Color Change and Mechanical Issues)
  Summarizing the root causes of our vital few
    By identifying variation of our causes
    Root cause analysis
Analyze-Step A0

## Slide 14
Analyze-Step A1
Detailed Process Map
Root Cause Analysis
Notes: 1. Addresses: What Does the Customer Want? What is a Good Product/Process? What is a Defect?
2. Goal of Performance Standard is to Translate the Customer Need into a MEASURABLE Characteristic.
3. Operational Definition is a Precise Description that Tells How to get a Value for the Characteristic You are Measuring.
To add or delete rows within this table, right-click and select “insert rows” or “delete rows”.

## Slide 15
Analyze-Step A2
Vital Few Identification
Pareto Analysis
82% Of scrap are due to:
Color Change(CC) procedure - 21 %
Mechanical (MECH)Issues – 19 %
Out of Specifications (OS) – 13 %
Start Up (SU) issues - 11 %
Contaminated Regrind(CR) – 9 %
Feed System Failure(FSF) – 9%
Regression Equation |  |  | 
Scrap = 706.534 + 0.978373 CC + 0.91847 MECH + 0.795376 OS + 0.883489 SU + 1.10903 CR + 1.01107 FSF |  |  | 
Coefficients |  |  | 
Term Coef SE Coef T P value |  |  | 
Constant706.534 155.355 4.54786 0.000 |  |  | 
CC 0.978 0.108 9.08724 0.000 |  |  | 
MECH 0.918 0.093 9.87326 0.000 |  |  | 
OS 0.795 0.106 7.53331 0.000 |  |  | 
SU 0.883 0.125 7.09266 0.000 |  |  | 
CR 1.109 0.127 8.72552 0.000 |  |  | 
FSF 1.011 0.136 7.40936 0.000 |  |  | 
Summary of Model |  |  | 
S = 810.594 R-Sq = 81.30% R-Sq(adj) = 80.13% |  |  | 
PRESS = 69633608 R-Sq(pred) = 79.35% |  |  | 
Regression Analysis
Notes: 1. Addresses: What Does the Customer Want? What is a Good Product/Process? What is a Defect?
2. Goal of Performance Standard is to Translate the Customer Need into a MEASURABLE Characteristic.
3. Operational Definition is a Precise Description that Tells How to get a Value for the Characteristic You are Measuring.
To add or delete rows within this table, right-click and select “insert rows” or “delete rows”.

## Slide 16
Conclusion from the Hypothesis Testing
Alternate hypothesis (: < There is a difference between the mean of scrap with “tested cause” and mean of scrap without “tested cause”>.
With α=0.05.Results with P value less than α are more significant.
The test produced the following P-values:
  Scrap vs. Scrap w.CC: 0.004
  Scrap vs. Scrap w.Mech 0.010
Chart: Difference w/o Scrap Cause
| CC* | MECH* | OS* | SU* | CR* | FSF*
Pounds | 717 | 631 | 460 | 375 | 304 | 301
Hypothesis Testing on vital few - T-Test
T-test conclusion
Analyze-Step A31

## Slide 17
List of Vital Few
Analyze-Step A4
Notes: Use this slide only if your data is continuous. Delete this page for Discrete Data sets.
Goal: Provide a visual/graphical display of the current process output data and determine whether your data is normal, which will dictate which analysis tools apply to your project. Some tools are based on your data being “normal” (such as the MSA you just completed in Step 3). See your BB/MBB coach for assistance.
To delete a sample chart or banner, use your mouse to select the item with one left click, right click and select ‘cut’ from the drop-down menu.
Populating the Minitab Graphic:
Select “Stat” from menu bar
Select “Basic Statistics” from pull down menu
Select “Display Descriptive Statistics” from pull down menu
Under “Variable”, with curser in box, double-click on column(s) containing data (output, Y, measures)
Click “Graphs” button (lower right corner) and check “Graphical Summary” and “OK” box
Click “OK” box again to calculate
Right click on graphic, choose “Copy Graph”; Right click in Power Point pitch page and select “Paste”
Enlarge by highlighting graphic (click once to get a box at each corner as needed) and go to a corner box to get a line with two arrows – Left click and drag out to desired size
Reposition to Center (Left click on image and drag to position)
Highlight/Circle Centering Tendencies and Standard Deviation

## Slide 18
Improve Step I0
Outcomes of Improve phase
Possible solutions to verified root causes
Evaluate and select best solution(low risk/high reward)
Pilot and test solutions.
  Actual key performance indicator Vs baseline test
Implement the optimized process model.
Notes: Examples of additional analysis tools. Minitab directions for populating follows.
To delete a sample chart or banner, use your mouse to select the item with one left click, right click and select ‘cut’ from the drop-down menu.
Minitab Box Plot:
select ‘Graph’ from menu bar, choose ‘Boxplot’ from drop-down menu
Left click once in ‘Y1’ field; double click on column name at left containing the data
Left click once in ‘X1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Histogram:
select ‘Graph’ from menu bar, choose ‘Histogram’ from drop-down menu
Left click once in ‘X1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Time Series Plot:
select ‘Graph’ from menu bar, choose ‘Time Series Plot’ from drop-down menu
Left click once in ‘Y1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Dot/Frequency Plot:
select ‘Graph’ from menu bar, choose ‘Dotplot’ from drop-down menu
Left click once in ‘Variables’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide

## Slide 19
Possible solutions
Improve Step I1
Problem |  |  | Vital Few |  | Root Causes |  | Solution |  | Data | 
 |  |  | Color Change(CC) |  | Changeover procedures |  | Changeover schedule by color |  | Scrap per color | 
 |  |  |  |  | Grindng at wrong grinder |  | Dedicate one Extruder to run white |  | (White,Yellow) | 
 |  |  |  |  | Grinder Trash |  | Grinding Matrix and training |  | Scrap per cause | 
 |  |  |  |  | Grinder connected to wrong silos |  |  |  | CR | 
Scrap |  |  | Color Change(CC) |  | Extruder type(Tandem vs Mixer & Cooler) |  | Convert E2 to tandem Extruder |  | Cause by Extruder | 
 |  |  | Mech |  | Running out of raw material(empty containers |  | More failure detection tools |  | CC on M/C vs Tandem | 
 |  |  |  |  | Feed System Failure,Clots ,raw material clumps) |  | (mistake proofing devices/Poke Yoke) |  | Extruder | 
 |  |  |  |  |  |  | PM program and training |  | Scrap by cause FSF | 
 |  |  |  |  | 6 heating zones on primary extruder |  | PM program |  | Scrap by Cause | 
 |  |  | Mech |  | Butane control system |  |  |  | Mech | 
 |  |  |  |  | Compressed air and chilling water supply system |  |  |  |  | 
Notes: Examples of additional analysis tools. Minitab directions for populating follows.
To delete a sample chart or banner, use your mouse to select the item with one left click, right click and select ‘cut’ from the drop-down menu.
Minitab Box Plot:
select ‘Graph’ from menu bar, choose ‘Boxplot’ from drop-down menu
Left click once in ‘Y1’ field; double click on column name at left containing the data
Left click once in ‘X1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Histogram:
select ‘Graph’ from menu bar, choose ‘Histogram’ from drop-down menu
Left click once in ‘X1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Time Series Plot:
select ‘Graph’ from menu bar, choose ‘Time Series Plot’ from drop-down menu
Left click once in ‘Y1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Dot/Frequency Plot:
select ‘Graph’ from menu bar, choose ‘Dotplot’ from drop-down menu
Left click once in ‘Variables’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide

## Slide 20
Best solutions
Improve Step I2
Impact/Effort & Cost Matrix
Notes: Examples of additional analysis tools. Minitab directions for populating follows.
To delete a sample chart or banner, use your mouse to select the item with one left click, right click and select ‘cut’ from the drop-down menu.
Minitab Box Plot:
select ‘Graph’ from menu bar, choose ‘Boxplot’ from drop-down menu
Left click once in ‘Y1’ field; double click on column name at left containing the data
Left click once in ‘X1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Histogram:
select ‘Graph’ from menu bar, choose ‘Histogram’ from drop-down menu
Left click once in ‘X1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Time Series Plot:
select ‘Graph’ from menu bar, choose ‘Time Series Plot’ from drop-down menu
Left click once in ‘Y1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Dot/Frequency Plot:
select ‘Graph’ from menu bar, choose ‘Dotplot’ from drop-down menu
Left click once in ‘Variables’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide

## Slide 21
Improve Step I3
Implement Solutions
Pilot and Implementation Activities
Notes: Examples of additional analysis tools. Minitab directions for populating follows.
To delete a sample chart or banner, use your mouse to select the item with one left click, right click and select ‘cut’ from the drop-down menu.
Minitab Box Plot:
select ‘Graph’ from menu bar, choose ‘Boxplot’ from drop-down menu
Left click once in ‘Y1’ field; double click on column name at left containing the data
Left click once in ‘X1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Histogram:
select ‘Graph’ from menu bar, choose ‘Histogram’ from drop-down menu
Left click once in ‘X1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Time Series Plot:
select ‘Graph’ from menu bar, choose ‘Time Series Plot’ from drop-down menu
Left click once in ‘Y1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Dot/Frequency Plot:
select ‘Graph’ from menu bar, choose ‘Dotplot’ from drop-down menu
Left click once in ‘Variables’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide

## Slide 22
Improve Step I4
Pilot and Test Solutions
Before & After Performance Assessment
Have I Reached My Goal?
Daily Extrusion Scrap decreased by 46 %
Notes: Examples of additional analysis tools. Minitab directions for populating follows.
To delete a sample chart or banner, use your mouse to select the item with one left click, right click and select ‘cut’ from the drop-down menu.
Minitab Box Plot:
select ‘Graph’ from menu bar, choose ‘Boxplot’ from drop-down menu
Left click once in ‘Y1’ field; double click on column name at left containing the data
Left click once in ‘X1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Histogram:
select ‘Graph’ from menu bar, choose ‘Histogram’ from drop-down menu
Left click once in ‘X1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Time Series Plot:
select ‘Graph’ from menu bar, choose ‘Time Series Plot’ from drop-down menu
Left click once in ‘Y1’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide
Minitab Dot/Frequency Plot:
select ‘Graph’ from menu bar, choose ‘Dotplot’ from drop-down menu
Left click once in ‘Variables’ field; double click on column name at left containing the data
click on ‘ok’; right click and select ‘Copy Graph’; right click and select ‘Paste’ in Power Point slide
use mouse to select graph and position on slide

## Slide 23
How Can I Sustain the Improvement?
Control Step C0
Outcomes of Control phase
Sustain the improvement:
control and monitoring plan control chart

## Slide 24
Defect | Measurement
Daily Extrusion Scrap(lbs) | Weight Scrap
How Can I Sustain the Improvement?
Has the business agreed to accept this process? YES
Who owns the new process? Ted Davis Extrusion Department Manager
Who runs the new process? Ted Davis and Extruder Operators
  Has this person(s) been properly trained? YES
Who monitors the new process and metrics? Ted Davis ,Extrusion Operators and QA Department
Turnover to the Business
Process Control
Control Step C1
Monitoring

## Slide 25
APPENDIX
Appendix
1 | Grinding Matrix
2 | Bi-weekly Changeover Schedule by color
3 | Annual PM Program
4 | Color wheel